QUIKRETE® Guide Specification

Exterior Use Anchoring Cement (No. 1245-81)

Rapid Setting, High Strength, Shrinkage Compensated Exterior Grade Anchoring Grout

Section 036100 – Cementitious Grouting

PART 1 – GENERAL

1.10	SUMMARY

A.  Provide rapid setting, high strength, shrinkage compensated exterior grade anchoring grout.

B.  Related Sections:  Other specification sections which relate directly to the work of this section

include the following:

Section 033000: Cast-In-Place Concrete

Section 034000: Pre-Cast Concrete

1.20	SUBMITTALS

A. 	Product Data:  Submit manufacturer’s product data and installation for each material and product

used. Include manufacturer’s Material Safety Data Sheets.

1.30	REFERENCES

A.  ASTM C 109: Compressive Strength of Hydraulic Mortars

B.  ASTM C 191: Setting Time of Hydraulic Cement

C.  ASTM E 488: Pull Out Strength of Anchors in Concrete and Masonry

1.40	QUALITY ASSURANCE

A.  	Manufacturer’s Qualifications: The manufacturer shall be a company with at least fifteen years

experience in the manufacturer and marketing of pre-packaged cementitious repair materials.

B.   Installer’s Qualifications:  The contractor shall be qualified to perform the work specified by reason

of experience.

1.50	DELIVERY, STORAGE AND HANDLING

A.  Deliver products in original packaging, labeled with product identification, manufacturer, batch

number and shelf life.

B.  Store products in a dry area.  Protect from direct sunlight.

C.  Handle products in accordance with manufacturer’s printed recommendations.

PART 2 – PRODUCTS

2.10	MATERIALS

A.  Rapid setting, high strength, shrinkage compensated exterior grade anchoring grout.

Comply with the following:

1.  Manufacturer:  Exterior Use Anchoring Cement (No. 1245-81), as manufactured by the

QUIKRETE® Companies, One Securities Centre, 3490 Piedmont Road, NE, Suite 1300,

Atlanta, GA 30305; telephone (404) 634-9100.

2.  Performance and Physical Properties at 73 degrees F (23ºC) and 50 percent relative humidity:

a. Compliance: ASTM C 928 R-2 specifications

b.  Setting time, ASTM C 191: 10-30 minutes

c. Compressive Strength, ASTM C 109: 2000 psi (13.8 MPa) @ 2 hours, 4000 psi (27.6 MPa)

@ 24 hours, 6000 psi (41.4 MPa) @ 7 days and 7000 psi (48.3 MPa) @ 28 days

d. Pull out Strength, ASTM E 488¹: 14,000 lb – force (6395 kg force) @ 24 hours, 21,000 lbs – force

(9571 kg – force) @ 28 days

¹ ASTMS E 488 Assembly: 1/2” (12 mm) threaded bolt embedded 8” (208 mm) in a 2” (50 mm) hole in 4,000 psi (27.6 MPa) concrete

PART 3 – EXECUTION

3.10	EXAMINATION

A.  Examine substrates and conditions under which materials will be installed. Do not proceed with

installation until unsatisfactory conditions are corrected.

B.  Coordinate installation with adjacent work to ensure proper sequence of construction. Protect

adjacent areas landscaping from contact due to mixing and handling of materials.

3.20	  SURFACE PREPARATION:

Comply with manufacturer’s printed instructions and the following:

1. Holes should be drilled at least 1” (25 mm) wider than the item to be anchored and a minimum of

2” – 4” (50-100 mm) deep.

2. Remove all loose concrete and debris from the hole.

3. Dampen the hole prior to pouring anchoring cement. Remove standing water.

3.30	  MIXING:

Comply with manufacturer’s printed instructions and the following:

- Add 5 parts Anchoring Cement with 1 part clean water.

2.  Pour powder into the water and mix vigorously until a flowable consistency is

achieved. For vertical applications reduce the amount of water for a putty – like

consistency.

3.  Mix only the amount of Anchoring cement that can be used in 10 minutes.

3.40	  APPLICATION:

Comply with manufacturer’s printed instructions and the following:

- Pour the mixed material into the hole or void to slightly above floor level.

2. Hold bolt or post in place until the material begins to stiffen.

3.50		CURING

A. No special procedures are required. During the first 24 hours, keep covered or damp

to prevent excessive loss of water.

3.60		CLEANING

A. Remove excess material before material cures. If material has cured, remove using

mechanical methods that will not damage substrate.

END OF SECTION