NON-SHRINK PRECISION GROUT

High strength, non-metallic, non-shrink grout designed for precision grouting and general construction applications.  Can be mixed to a plastic, flowable or fluid consistency.  

Use For:
• Grouting heavy equipment, pre-cast concrete, bearing plates, steel columns and anchoring applications

Compressive Strength at 28 Days

Plastic
14,000 psi
96.5 MPa

Flowable
12,000 psi
86.2 MPa

Fluid
8,000 psi
55.2 MPa
Complies with ASTM C 1107 and Army Corp of Engineers CRD 621
